SPECTROPHOTOMETRIC DETERMINATION OF ION RELEASE FROM DENTAL AMALGAM IN DIFFERENT LIQUID MEDIA

M. Kakalova*, I. Stamatova**, G. Bekjarov*, S. Vladimirov**

* Canning Research Institute – Plovdiv

** Medical University Plovdiv, Department of Operative Dentistry and Endodontics

Abstract: Aim: Safety issue of amalgam remains yet controversial. The aim of this study was to determine the metals released from amalgam samples in various liquid media.

Material and methods: Ten samples per seven study groups were prepared in plastic molds with diameter 5.8 mm and height 4 mm. Two hours after setting at room temperature the cylindrical samples were immersed in test liquids and kept for 24 and 48 hours, respectively. Metal releases in liquid medium were measured by atomic emission spectrometer with inductive coupled plasma.

Results: There was a time-dependent decrease in Hg, Cu and Ag release. The obtained results are present in table below.

Table1. Content of the  elements in mg/l after 24h immersion of amalgam in different liquids

| Liquid | Cu | Zn | Ag | Hg |
| --- | --- | --- | --- | --- |
|  | X ± Sx | X ± Sx | X ± Sx | X ± Sx |
| Deionised water | < 0.003 | 0.25 ± 0.02 | < 0.003 | 0.13 ± 0.03 |
| 17% EDTA | < 0.003 | 1.20 ± 0.04 | < 0.003 | 0.17 ± 0.04 |
| 0.9% NaCl | < 0.003 | 0.24 ± 0.02 | < 0.003 | 0.12 ± 0.04 |
| 4% CH3COOH | 0.010 ± 0.004 | 1.25 ± 0.03 | < 0.003 | 0.10 ± 0.02 |
| Sprite | < 0.003 | 1.48 ± 0.05 | < 0.003 | 0.15 ± 0.04 |
| Coca-Cola light | 0.026 ± 0.007 | 4.15 ± 0.05 | 0.029 ± 0.004 | 0.18 ± 0.05 |
| Red wine-Mavrid | < 0.003 | 1.72 ± 0.02 | 0.040 ± 0.006 | 0.10 ± 0.02 |

Table2. Content of the elements in mg/l after 48h immersion of amalgam in different liquids

| Liquid | Cu | Zn | Ag | Hg |
| --- | --- | --- | --- | --- |
|  | X ± Sx | X ± Sx | X ± Sx | X ± Sx |
| Deionised water | < 0.003 | 2.10 ± 0.08 | < 0.003 | 0.10 ± 0.03 |
| 17% EDTA | 0.009 ± 0.004 | 0.22 ± 0.02 | < 0.003 | 0.09 ± 0.02 |
| 0.9% NaCl | 0.007 ± 0.003 | 0.99 ± 0.03 | < 0.003 | 0.17 ± 0.04 |
| 4% CH3COOH | 0.010 ± 0.004 | 0.37 ± 0.02 | < 0.003 | 0.10 ± 0.02 |
| Sprite | < 0.003 | 0.26 ± 0.02 | < 0.003 | 0.09 ± 0.03 |
| Coca-Cola light | 0.009 ± 0.004 | 1.44 ± 0.07 | 0.008 ± 0.002 | 0.12 ± 0.02 |
| Red wine-Mavrid | < 0.003 | 0.40 ± 0.03 | 0.036 ± 0.005 | 0.09 ± 0.03 |

* Full text of publication in Dental Medicine, 2008, No1, p. 30-33